PAINTFACTOR DOCTRINE

Window Systems Painting

Substrate Preparation, Application Methodology,

and Industry Standard Compliance

Version 1.0 DRAFT

January 2026

Source: NotebookLM Research Report

Comprehensive Technical Manual for Professional Architectural

Coating of Residential Window Systems

# 1. Introduction and Scope

Window painting represents one of the most technically demanding segments of architectural finishing. Unlike broad wall surfaces, windows are complex mechanical assemblies composed of diverse substrates requiring specialized preparation and application protocols. This doctrine establishes the technical standards for window system coating within PaintFactor specifications.

## 1.1 Governing Standards

All window painting specifications shall comply with PCA (Painting Contractors Association) Industry Standards P1 through P25 and AAMA (American Architectural Manufacturers Association) performance specifications for metallic substrates.

## 1.2 Definition of Properly Painted Surface

Per PCA/FCA unified standards, a properly painted surface exhibits uniform appearance in color, texture, hiding, and sheen. The film shall be virtually free of foreign material, lumps, skins, runs, sags, holidays, and misses. Surrounding environment shall be free of drips, spatters, spills, or overspray.

### 1.2.1 Inspection Protocol

- Inspection distance: 39 inches (1 meter) minimum, without magnification

- Lighting: Finished lighting conditions (as occupied)

- Position: Normal viewing position (eye level)

# 2. PCA Industry Standards Reference

The following PCA standards govern window painting contracts and quality expectations:

| Standard | Subject Matter and Application |
| --- | --- |
| PCA P1 | Definition of Properly Painted Surface; touch-up and damage repair protocols |
| PCA P2 | Third-party inspector qualifications and responsibilities |
| PCA P3 | Cost impact of multiple colors and finish types (estimation relevance) |
| PCA P4 | Surface inspection and approval responsibility prior to coating |
| PCA P5 | Benchmark sample submission and approval protocols |
| PCA P7 | Order of work between trades |
| PCA P9 | Trade terminology definitions for scope of work |
| PCA P14 | Surface preparation levels for repainting/maintenance |
| PCA P24 | Spot repair inspection and acceptance procedures |

# 3. Wood Window Systems

Wood remains predominant in high-end residential construction due to thermal efficiency and aesthetic versatility. Its hygroscopic nature requires careful moisture management to prevent dimensional instability and biological decay.

## 3.1 Moisture Requirements

Maximum Moisture Content: 19% before painting

Interior Joinery (heated): 6% to 8% MC

Exterior Envelope: 9% to 14% MC

### 3.1.1 Testing Methods

- Pin-type meters: Measure electrical resistance at depth

- Pin-less meters: Non-destructive surface readings

- Pencil test: For "dozy" wood (soft/rotting fibers), determines decay depth

Soft or rotted wood must be removed and replaced with new timber sections or professional joiner splices before painting can proceed.

## 3.2 Sanding Sequence

The Golden Rule: Never skip more than one grit in a sequence. This ensures scratches from the previous grit are effectively leveled.

| Stage | Grit | Purpose |
| --- | --- | --- |
| Initial Stripping | 60-80 | Heavy removal of failed/peeling paint, thick varnish |
| Smoothing | 100-120 | Leveling surface, removing post-strip imperfections |
| Pre-Primer | 150-180 | Smoothing grain for initial coating (polyurethane/enamel) |
| Final Surface Prep | 220 | Final sand of bare wood before primer; ensures even absorption (QT-4 and up) |
| Between-Coat Scuff | 320 | Smoothing primer/first coat; removes raised fibers (nibs) (QT-4 and up) |

### 3.2.1 Wood Species Considerations

- Softwoods (pine, alder): Start at 120 grit, finish at 220 (water-based) or 180 (oil-based)

- Hardwoods (oak, maple): Final sand at 150-180 grit to prevent burnishing

# 4. Muntin and Glass Interface Techniques

Muntins (narrow wood strips separating panes) represent the most labor-intensive window painting component, requiring both precision and weather-sealing strategy.

## 4.1 The 1/16-Inch Seal Technique

Professional contractors apply paint slightly onto the glass pane by approximately 1/16 inch. This is not a mistake but a functional requirement that creates an airtight seal between glass and wood/glazing putty, preventing moisture infiltration and premature rot.

### 4.1.1 Execution Protocol

- Cut in paint overlapping glass by 1/16 inch

- Allow paint to fully dry

- Score a straight line on glass using sharp razor blade with putty knife guide

- Scrape away excess paint from glass

## 4.2 Liquid Masking Technology

Liquid masking agents (e.g., Masking Liquid H2O, Jasco Mask & Peel) provide significant efficiency gains for multi-pane Colonial-style windows.

### 4.2.1 Application Process

- Apply liquid mask liberally to glass and sash parts (acts as primer for wood, peelable film for glass)

- Paint topcoats directly over mask and frame

- Once dry, score edge of glass with utility knife

- Peel mask away for crisp line and clean glass

Limitation: Avoid liquid masks on weathered, dry wood which requires deep-penetrating oil-based primer.

# 5. Vinyl and PVC Window Systems

Vinyl (uPVC) is a thermoplastic sensitive to heat absorption. Dark exterior colors can cause warping, buckling, and insulated glass seal failure without proper coating technology.

## 5.1 Light Reflectance Value (LRV) Requirements

Standard Practice: Only colors with LRV ≥ 55 should be applied to vinyl frames

Dark colors (low LRV) absorb solar energy, raising substrate temperature beyond structural limits.

### 5.1.1 Vinyl-Safe Technology

For dark colors (black, deep bronze), use vinyl-safe paint lines with heat-reflective pigments that reflect infrared radiation while appearing dark to visible spectrum.

- Sherwin-Williams Emerald Urethane Trim Enamel (vinyl-safe color deck)

- Benjamin Moore Aura Exterior (vinyl-safe colors)

## 5.2 Adhesion Protocol for Non-Porous Polymers

- Cleaning: TSP substitute or mild detergent, followed by 70%-91% isopropyl alcohol wipe to eliminate silicone residues

- Etching: Light scuff-sand with 220-grit to create micro-tooth for primer

- Priming: Adhesive bonding primer rated for vinyl/PVC (INSL-X STIX, Sherwin-Williams Extreme Bond)

# 6. Aluminum Window Systems

Aluminum windows require industrial-grade preparation to manage oxidation and ensure long-term durability.

## 6.1 Chemical Pre-treatment

- BC-7000 or equivalent heavy-duty alkaline cleaner for degreasing

- Concentrated solutions may act as etchants for primer adhesion

- Organofunctional silanes and organometallic compounds (zirconium/titanium-based) create chemical bonds between metal surface and paint resin

## 6.2 AAMA Performance Specifications

Industry standards for aluminum window coatings are set by AAMA (now part of Fenestration and Glazing Industry Alliance).

| Specification | Target Use | Weathering | Performance |
| --- | --- | --- | --- |
| AAMA 2603 | Interior/Low-Exposure | 1 Year South FL | Slight fade/chalk resistance |
| AAMA 2604 | High-Performance | 5 Year South FL | 30% gloss; <5 Delta E fade |
| AAMA 2605 | Superior Performance | 10 Year South FL | 50% gloss; <5 Delta E fade |

Recommended Product: Polane Solar Reflective Polyurethane Enamel for industrial-grade UV and mar resistance.

# 7. Window Estimation: Opening Count Method

The Opening Count Method simplifies window estimation but requires dimensional adjustments and complexity multipliers.

## 7.1 Core Principles

### 7.1.1 Dimensional Adjustments

Windows are not counted as simple "1 opening" units. For wood windows: count 1 opening per 6 square feet of window area.

Example: A standard 6 SF window = 1 opening; a 24 SF picture window = 4 openings

### 7.1.2 Complexity Multipliers

| Window Type | Opening Value | Rationale |
| --- | --- | --- |
| French Doors/Windows | 1.5 openings | Divided lights |
| Dutch Doors | 2.0 openings | Split configuration |
| Paneled (vs. Flush) | 1.25 openings | Panel detailing |

### 7.1.3 Method Limitations

- Designed primarily for interior paint-grade work

- Exterior doors require separate per-door method for weatherproofing systems

- Oddly shaped windows or window walls may require reversion to SF calculations

# 8. Application Methodology

## 8.1 Brush vs. Spray Decision Framework

### 8.1.1 Manual Brushing

- Provides unparalleled control for detailed trim and muntins

- 1.5-inch angled sash brush works paint into grain and complex profiles

- Labor-intensive; may leave brush marks/texture

### 8.1.2 Spray Systems (HVLP/Air-Assisted Airless)

- Factory-like smooth finish; significantly faster for large surfaces

- 15-Square-Meter Rule: Spraying becomes more efficient above 15 m² despite setup time

- Waste Factor: 20%-40% material waste from overspray and box method (50% overlap)

- Requires extensive masking and containment

## 8.2 Productivity Metrics

| Window Type | Labor Factor | Notes |
| --- | --- | --- |
| Double-Hung (Basic) | 1.10-1.25 hrs/ea | Standard prep and two coats |
| Casement | 1.10 hrs/ea | Similar to DH; easier access |
| Colonial (Multi-pane) | 1.10 × 1.20 | +20% for muntin complexity |
| Windowsills | 0.06 hrs/LM | Linear measurement for horizontals |

Height Factor: Second-story windows requiring scaffolding can double or triple labor hours.

# 9. Film Thickness and Curing

## 9.1 Film Build Requirements

Coating performance is fundamentally tied to film build. Too thin: insufficient UV blockers and protective resins. Too thick: curing failure leading to blocking or softness.

### 9.1.1 DFT Calculation

DFT = WFT × (% Volume Solids)

Example: 34% volume solids at 3 mils WFT = 1.02 mils DFT

Target System DFT: Minimum 2.5 mils; maximum 5 mils (to prevent internal stress/cracking)

## 9.2 Measurement Tools by Substrate

| Tool | Substrate | Mechanism |
| --- | --- | --- |
| WFT Gauge (Comb) | All (while wet) | Measures liquid depth immediately after application |
| Magnetic Induction | Ferrous Metal (Steel) | Magnetic flux change measures non-magnetic coating |
| Eddy Current | Non-Ferrous (Aluminum) | Electromagnetic induction on conductive metal |
| Ultrasonic (PosiTector) | Wood / Vinyl | Times ultrasonic pulse reflections from substrate |

# 10. Common Defects and Remediation

## 10.1 Blocking and Sticking

Occurs when freshly painted surfaces stick together when pressed (closing window before full cure).

### 10.1.1 Causes

- Application in high humidity

- Low-quality vinyl-acrylic latex

- Insufficient cure time (often 3-7 days for enamels)

### 10.1.2 Prevention

- Use 100% acrylic or urethane-enriched enamels

- Paint sashes in "ajar" position

- Avoid painting sliding pulley stiles or meeting rails

### 10.1.3 Remediation

Sand to dull finish, prime with high-block-resistant primer, repaint.

## 10.2 Bridging and Pinholing

Bridging: Coating spans a gap without filling it, creating hollow void that eventually cracks. Caused by excessive paint viscosity or improper technique.

Pinholing: Tiny blisters from trapped air, solvent, or moisture escaping during cure. Caused by inadequate substrate cleaning, ignoring flash-off times, or application in direct intense sunlight.

## 10.3 Metallic Coating Defects

Bleeding or shading in metallic/pearlescent finishes caused by uneven orientation of aluminum flakes.

### 10.3.1 Solutions

- Maintain consistent spray distance

- Use faster-evaporating thinners in cold conditions

- Thoroughly mix metallic pigments

# 11. Lead RRP Compliance

For residential structures built before 1978, the EPA Renovation, Repair, and Painting (RRP) Rule governs window projects. Window work is categorized as high-risk due to friction surfaces (sashes sliding in frames) being major lead dust generators.

## 11.1 Lead-Safe Work Practices

### 11.1.1 Required Protocols

- Notification: Provide "Renovate Right" pamphlet to owner at least 7 days prior to work

- Containment: Interior areas sealed with plastic; exterior protection extends 10 feet from building with wind protection

- Cleanup: HEPA vacuum and wet-mop sequence, followed by clearance dust-wipe test by licensed inspector

### 11.1.2 Prohibited Acts

- Open-flame torches

- Heat guns above 1100°F

- Power-sanding without HEPA vacuum attachment

## 11.2 VOC Compliance

Modern window coatings must comply with regional VOC regulations (e.g., SCAQMD in California). High-performance water-based urethanes provide alkyd durability with lower environmental impact and faster return-to-service times.

# 12. Lifecycle Management

## 12.1 Climate-Based Considerations

### 12.1.1 Coastal Environments

- Most severe conditions: salt spray, high humidity, UV exposure

- Application window: late spring through early fall only

- Inspect every 2 years; rinse annually with fresh water

### 12.1.2 Southwest/Desert

- Extreme thermal cycling (10°F-20°F swings in hours)

- Requires flexible or elastomeric topcoats that expand/contract without micro-cracking

## 12.2 Warranty and Recoat Intervals

- Manufacturer recommendation: exterior recoat every 2-3 years for warranty validity

- High-quality two-coat system: 7-15 years on stable substrates

- South/West-facing elevations weather faster than North/shaded elevations

# 13. PaintFactor Integration Notes

The following considerations apply when integrating window painting specifications into the PaintFactor estimation system.

## 13.1 Specification Structure

- Window specifications consume geometry from PaintScope (EA counts, dimensions)

- Substrate type determines preparation protocol and primer selection

- Window style (double-hung, casement, colonial) drives complexity modifiers

- Quality tier (QT3-QT6) determines coating system and production rate adjustments

## 13.2 Modifier Categories

- Substrate: Wood, vinyl, aluminum (affects prep and primer)

- Condition: New, recoat, deteriorated (affects prep labor)

- Style: Basic, colonial/multi-pane, French (+20% to +50% labor)

- Access: Ground level, ladder, scaffold (height multiplier)

- Lead: Pre-1978 structures require RRP protocol modifier

## 13.3 Estimation Engine Considerations

- Opening Count Method provides baseline for interior paint-grade work

- Large windows (>6 SF) scale by SF/6 for accurate opening equivalents

- Exterior weatherproofing requires separate calculation from interior work

- Material coverage varies significantly by application method (brush vs. spray waste factor)

--- End of Doctrine Document ---